|  |  |  |  |
| --- | --- | --- | --- |
| **Photo**  **of the analysed area** | **Analyzed area** | **Concentration (%w.w)** | |
| **Cu** | **Sn** |
|  | 2a | 89.2 ± 1.0 | 9.82 ± 0.5 |
|  | 2b | 92.5 ± 1.0 | 6.32 ± 0.3 |
|  | 2c | 81.9 ± 1.0 | 16.4 ± 0.8 |
| Table 2: Elemental composition of the base bronze metal for Baal God figurine. Although all analyzed areas look similar, only the area 2b was screened to represent best the true alloy surface providing quantitative results representative of the original alloy composition. | | | |